Publication is available for discussion in the framework of on-line conference “Butlerov readings”. http://butlerov.com/readings/

Contributed to editorial board: December 31, 2010.

Subject area: Manufacturing of synthetic motor fuels.

Indirect alkylation of isobutane by bioalcohol on the hybrid

catalyst with production of high-octane fuels

© Rishat R. Shiriyazdanov ,1*+ Artur R. Davletshin,2+ and Ekaterina A. Ipatova3

1 Faculty technologies of oil and gas. SEC “Catalytic systems and nanomaterials in the processing of fossil and renewable hydrocarbons raw”. Ufa state petroleum technical university.

Cosmonauts St., 1. Ufa, 450062. Russia. Republic of  Bashkortostan.

Phone: +7 (347) 243-15-35. E-mail: petroleum9@bk.ru

2 Fuel process division. Institute of petroleum refining and petrochemistry.

SEC “Catalytic systems and nanomaterials in the processing of fossil and renewable hydrocarbons raw”.

Ufa state petroleum technical university. Iniciativnaya St., 12. Ufa, 450065. Russia.

Republic of  Bashkortostan. Phone: +7 (347) 242-24-73. E-mail: davletshinar@list.ru

3 SEC “Catalytic systems and nanomaterials in the processing of fossil and renewable hydrocarbons raw”. Ufa state petroleum technical university. Cosmonauts St., 1. Ufa, 450062. Russia. Republic of Bashkortostan.

Phone: +7 (347) 223-79-85. E-mail: ipatovaea@bashneft.ru

___________________________________

*Supervising author; +Corresponding author

Keywords: biobutanol, bioethanol, isobutene, indirect alkylation, montmorillonite, anion-modified metal oxide.

Abstract

On the example of conversion of biobutanol and bioethanol with isobutane on the hybrid catalyst prepared by mechanical synthesis of montmorillonite and an anion-modified metal oxide there have been shown the principal possibility of joint processing of alternative raw materials with biomass-based, involving hydrocarbons of associated petroleum gas or refinery gas with production of high-octane fuels.