Publication is available for discussion in the Internet as a material of “All-Russian Working
                                                                  Chemical Conference “Butlerov’s Heritage-2011”. http://butlerov.com/bh-2011/

Contributed to editorial board: March 22, 2011.

The accumulation of mechanical blow energy

by the crystal lattice of inorganic compounds

© Ismail A. Massalimov,1,2+* Airat U. Shayakhmetov,2 Ahat G. Mustafin,1 and Rita Z. Usmanova2

1 Bashkir State University. Zaki Validi St., 32. Ufa, 450074. Bashkortostan Republic. Russia.

Phone: +7 (347) 273-67-27. E-mail: ismail_mass@mail.ru.

2 Research Technological Institute of Herbicides and Plant Growth Regulators of the Academy of Sciences. Ulyanovykh St., 65. Ufa, 450029. Bashkortostan Republic. Russia.

Phone: +7 (347) 242-76-53.  E-mail: mag@anrb.ru.

___________________________________

*Supervising author; +Corresponding author

Keywords: mechanical activation, centrifugal crusher, excess enthalpy, differential thermal analysis (DTA).

Abstract

The results of thermal study of mechanically activated in centrifugal crusher of inorganic materials with different type of chemical bond are presented. It is established that intensive mechanical leads to accumulation of excess enthalpy in matter with covalent and ionic-covalent bonds in the form of sharp exothermal peaks on the differential thermal analysis curve. It is found that intensity and shape of exothermal peaks depend on nature of activated matter and duration of treatment. Results of study can be used during action of technological process with using mechanically activated chemicals.