Publication is available for discussion in the framework of the on-line Internet conference “*Butlerov readings*”. http://butlerov.com/readings/

Submitted on November 02, 2017.

**Investigation of nonmetallic inclusions and the**

**structure of pipe steel microalloyed with boron**

©**Anatoly A. Babenco**,\* **Natalia I. Selmensky**,and **Alena G. Upolovnikova**+

*Laboratory of Pyrometallurgy of Non-Ferrous Vetals. Institute of Metallurgy of the UB of the RAS.*

*Amundsen St., 101. Ekaterinburg, 620016. Sverdlovsk Region. Russia.*

*Phone: +7 (343) 232-90-24. E-mail: upol.ru@mail.ru*

\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_

\*Supervising author; +Corresponding author

***Keywords:*** pipe steel, boron, sulfur, manganese, non-metallic inclusions, structure, mechanical properties.

**Abstract**

A study of the amount and composition of nonmetallic inclusions showed that when boron is introduced, the volume fraction of oxide and oxysulfide inclusions increases and the volume fraction of sulfide inclusions significantly decreases. At the same time steel alloying by boron increases the proportion of inclusions up to 98.7% with a size of no more than 5 microns, compared with 80.6% in the comparative metal. In the experimental metal, the proportion of nonmetallic inclusions larger than 10 μm does not exceed 0.6%, compared to 13.6% in a metal without boron. Studies of nonmetallic inclusions showed that in an experimental metal containing 0.006% boron, independent boron containing inclusions were not detected. Boron was not found in the composition of the investigated nonmetallic inclusions. In the samples of rolled metal for experimental and comparative melting, nonmetallic inclusions are predominantly oxides, oxysulfide and sulfide inclusions. The phase composition of nonmetallic inclusions in a comparative sample without boron, containing in % mass.: 1.4 Mn and 0.005 S, is represented by oxide and oxysulfide inclusions of complex composition and separate sulphide inclusions. In the experimental sample of pipe steel containing in mass%: 0.006 B, 1.4 Mn and 0.003 S, the most common are small inclusions having in 99% of cases a size of not more than 5 μm and represented by a large number of silicate glasses with iron and manganese oxides 1-2 μm in size and round oxysulfides. The steel microalloying by boron is accompanied by the formation of a dispersed ferritic-bainite structure, which consists of fine-grained ferrite with bainite sites. The increase in the dispersion of the structure of the experimental steel sample is indicated by the decrease in the size of the ferritic grain from 8.7 to 7.2 microns. The microalloying of pipe steel by boron practically did not affect the size of the austenite grain. The microhardness of ferrite and perlite, in the comparative steel sample without boron, does not exceed 180 and 214 HV10, respectively. The presence of boron in the test steel sample in an amount of 0.006% increases the microhardness of ferrite to 260 HV10 and bainite to 314 HV10. This is due to the fact that boron, being a sufficiently active element, segregates first at the interphase boundaries. This contributes to an increase in the concentration and uniformity of the distribution of carbon in the volume of grains and leads to an increase in the dispersity and hardness of the experimental metal structures under study.

**References**

1. V.L. Pilyushenko, V.A. Vihlevschuk. Scientific and technological bases of microalloying steel. *Moscow: Metallurgy.* **2000**. 384p. (russian)
2. V.A. Golubcov, V.V. Lunev. Modification of steel castings and ingots. *Chelyabinsk - Zaporozhye: ZNTU.* **2008**. 356p. (russian)
3. Y.G. Goldstein, V.G. Mizin. Modification and microalloying of iron and steel. *Moscow: Metallurgiya.* **1986**. 271p. (russian)
4. Boron, calcium, niobium and zirconium in the cast iron and steel. Edited by Vinarov S.M. *Moscow: State scientific and technical publishing literature on ferrous and non-ferrous metallurgy.* **1961**. 459p. (russian)
5. M.V. Bobylev, E.G. Koroleva, A.M. Shtannikov. Future economy alloyed boron steel for the production of high-strength fixing details. *Metal Science and Heat Treatment of Metal.* **2005**. No.5. P.51-55. (russian)
6. A.B. Sychkov, V.V. Parusov, A.M. Nesterenko, M.A. Zhigarev. Structure and properties of wire rod from boron-containing steels, intended for the production of welding wire. *Metallurgical and mining industry*. **2000**. No.3. P.48-51. (russian)
7. G.V. Levchenko, A.I. Yatsenko, N.I. Repina. Testing the technology of production of thin-sheet low-carbon steel, micro-alloyed boron. *Metallurgical and mining industry.* **2003**. No.1. P.56-59. (russian)
8. N.P. Lyakishev, Yu.L. Pliner, S.I. Lappo. Boron steels and alloys. *Moscow: Metallurgiya.* **1986**. 192p. (russian)
9. A.A. Babenko, V.I. Zhuchkov, L.I. Leont'ev and etc. Microalloying boron steel - a promising way to improve the competitiveness of domestic steel. In.: Proceedings of the scientific - practical conference "Prospects of development of metallurgy and machine building with completed basic research and R & D", 2013, Ekaterinburg. *Ekaterinburg: "UIPTS" OOO.* **2013**. P.162-165. (russian)
10. E.M. Krivko, P.I. Chub, R.P. Konovalov. Microalloying of boiling steel with boron during its reduction from oxides. Casting steel into molds: Sb.nauch.tr. NCHM SSSR. *Moscow: Metallurgy.* **1984**. P. 24-25. (russian)
11. A.A. Babenko, V.I. Zhuchkov, L.A. Smirnov and etc. Research and development of complex manufacturing techniques of low carbon boron steel with low sulfur content. *Steel.* **2015**. No.11. P.48-50. (russian)
12. C.J. Heckmann, D. Ormston, et. al. Development of low carbon Nb-Ti-B microalloyed steels for high strength large diameter linepipe. *IronandSteelmaking.* **2005**. No.4. P.57- 60.
13. *Patent No. 6 228 183 US, IPC 7 C22C38. 04, C22C38. 06, C22C38. 12, C22C38. 14.* Ultra-high strength, weldable, boron-containing steels with superior toughness. Bangaru Narasimha-Rao V; Koo Jayoung; Luton Michael J at all. Declared on July 28. **1997**; publ. 08.05.01. 14p.
14. H. Asahi, T. Haara, E. Tzuru and others. The development of ultrahigh-strength pipes X120 UEO. International seminar "Modern steels for gas and oil pipes, problems and prospects": coll. reports. *Moscow: Metallurgizdat.* **2006**. P.123-130. (russian)
15. Technological instruction TI SK-01-2007 "Melting of steel in oxygen converters". *Temirtau. JSC ArcelorMittal Temirtau.* **2007**. (russian)
16. Technological instruction TI SK-07-2007 "Out-of-furnace processing of steel for slab caster". *Temiratau.* *JSC ArcelorMittal Temirtau.* **2007**. (russian)
17. *Patent № 2562849* "Slag mixture for processing steel in a ladle" Babenko A.A., Zhuchkov V.I., Selivanov E.N., Sychev A.V., Zolin A.N., Dobromilov A.A., Kutdusova X.Sh., Savrasov A.I., Kim A.S., Akberdin A.A. Published by Bul. №25 of 10.09.**2015**. (russian)
18. A.A. Babenko, V.I. Zhuchkov, E.N. Selivanov, A.V. Sychev. The slag mixture for processing is cast in a ladle. Pat. No. 30964 (*Republic of Kazakhstan*) **2016**.